Sequence-selective assembly of tweezer-molecules on linear templates enables frameshift-reading of sequence information

Zhixue Zhu, Christine J. Cardin, Yu Gan and Howard M. Colquhoun*

Department of Chemistry, University of Reading, Whiteknights, Reading, RG6 6AD, UK

Email: h.m.colquhoun@rdg.ac.uk;  Tel: (+)44 (0)118 378 6717

Abstract:  Monomer-sequence information in synthetic copolyimides can be recognised by tweezer-type molecules binding to adjacent triplet-sequences on the polymer chains. In the present paper different tweezer-molecules are found to have different sequence-selectivities, as demonstrated in solution by 1H NMR spectroscopy and in the solid state by single crystal X-ray analyses of tweezer-complexes with linear and macrocyclic oligo-imides. This work provides clear-cut confirmation of polyimide chain-folding and adjacent-tweezer-binding. It also reveals a new and entirely unexpected mechanism for sequence-recognition which, by analogy with a related process in biomolecular information processing, may be termed "frameshift-reading". The ability of one particular tweezer-molecule to detect, with exceptionally high sensitivity, long-range sequence-information in chain-folding aromatic copolyimides, is readily explained by this novel process.

The idea that digital information might be encoded at the molecular level, as a linear sequence of monomer residues in a copolymer chain, first crystallised some fifty years ago with discovery of the structure,, and function of DNA; a linear, high molecular weight organopolyphosphate in which the information represented by its nucleotide monomer-sequences was found to ultimately specify the amino acid sequences of proteins. Viewed purely as digital information however, DNA – with its four co-monomers – is far more complex than strictly necessary, since even the simplest two-monomer copolymer is the logical equivalent of a string of binary numbers. It is significant that, in biology, no specific information is ever written to DNA: random copying errors may be captured by evolution, but the key problem - solved in Life by the operation of a dauntingly intricate set of molecular machinery – is how comonomer  sequences are to be read.

We, and others,, have recently begun to explore the possibility that synthetic copolymers might, in principle, be used to store and process digital information. Several groups have described the development of small, -electron-rich, aromatic tweezer-molecules,,,,,,,,, and we have recently shown that certain molecules of this type can recognise and bind to specific triplet sequences in high molecular weight aromatic co-polyimides.,,, Binding occurs via sterically- and electronically-complementary --stacking,,,,,,,, and hydrogen-bonding between the tweezer-molecules and monomer residues (Fig.1). As in many supramolecular systems where aromatic --stacking plays a key role,,,,,,,,, this interaction results in very large, ring-current-induced complexation shifts of 1H NMR resonances arising from the associating components, here involving triplet binding sequences.19,20 Moreover, NMR data for a range of copolymers show that the tweezer-molecules are able to "read" sequences which are more extended than simple triplets, by a mechanism which we have suggested may involve polymer chain-folding and multiple adjacent tweezer-binding.21 In the presence of the tweezer, co-monomer sequences in which two, one, or no tweezer-molecules can be bound at sequences adjacent to the central diimide binding site are found to give three separate diimide resonances.21 Adjacent tweezer-binding to a chain-folded polyimide (Fig. 1) would produce additional ring-current shielding of the "observed" diimide protons (highlighted in blue), so providing a possible mechanism for detection of extended sequence-information.

Figure 1 (  Proposed19,20,21 chain folding of a polyimide-sulfone and multiple tweezer-binding at adjacent triplet sequences. Defining the diarylene-pyromellitimide unit as "I" and the bis(arylsulfonyl)-4,4'-biphenylene residue as "S", each tweezer-molecule binds to the triplet monomer-sequence "SIS". (Note: adjacent triplets are overlapping, since each "S" residue interacts with two tweezer-molecules.

Here we report the synthesis and characterisation (both in solution and, crystallographically, in the solid-state) of discrete complexes between tweezer-molecules and fully-defined diimide oligomers, both linear and macrocyclic. This work finally validates the hypothesis of polyimide chain-folding and adjacent-tweezer-binding, and also reveals a novel mechanism for sequence-recogition which, by analogy with a related process in biomolecular information-processing, we term "frameshift-reading". This wholly unexpected result explains, for the first time, the ability of one particular tweezer-molecule to detect, with extraordinarily high sensitivity (see ESI), long-range sequence-information in chain-folding aromatic copolyimides.22

Results and discussion

Diimide oligomers 1, 2 and 3 were synthesised by chemical imidisation of mixtures of diamine 4 and the end-capping monoamine 5 with either pyromellitic dianhydride (for 1) or 1,4,5,8-naphthalenetetracarboxylic dianhydride (for 2 and 3), in the presence of acetic anhydride. The products were fractionated by column chromatography to afford pure, single oligomers. Attempts to grow diffraction-quality single crystals of complexes between these oligomers and the previously-reported tweezer-molecules 6 and 7 were unsuccessful, but a new type of tweezer, (8), containing a ferrocenyl substituent (but with an otherwise similar structure to tweezer-molecule 6), ultimately gave well-formed crystals of a 2:1 complex with oligo-imide 1. The X-ray structure of [82+1] is shown in Fig. 2, from which it is evident that the previously-hypothesised19,20,21 adjacent binding of tweezer-molecules does indeed occur. In [82+1] the two tweezer-molecules are related by a crystallographic inversion centre, and bind to the terminal diimide residues of the oligomer. Chain-folding of the oligomer leads to formation of a multiple -stack comprising seven electronically-complementary components (four electron-rich tweezer-arms, two electron-deficient pyromellitimide residues and one electron-deficient 4,4'-biphenylenedisulfone unit). A strong hydrogen bond (N-H...O=C = 2.26 Å, (N-H…O = 173°) is found between each tweezer-molecule and a carbonyl group of its bound pyromellitimide residue.

Figure 2 (  X-ray structure (two views) of the 2:1 complex [82+1] between the ferrocenyl tweezer-molecule 8 and the bis-pyromellitimde oligomer 1. Tweezer-molecules are shown in blue to distinguish the three components of the assembly, with intermolecular hydrogen bonds (N-H…O=C) in magenta.

The perpendicular distance in the crystal between each proton of a pyromellitimide residue and the mean plane of a non-adjacent pyrenyl ring (c.f. Fig. 2) is ca. 10.5 Å, very close to the value of 10.8 Å predicted by an earlier computational modelling study of the corresponding tweezer-polymer complex.21 This brings the diimide protons well within the "0.1 ppm shielding radius" of the adjacently-bound pyrenyl residue, calculated at ca. 12.0 Å. Consequently, in addition to the large complexation shift of the diimide resonance resulting from tweezer-binding at the diimide unit, additional upfield shifts of the diimide resonance are predicted (and observed) when tweezer-binding is possible at one or both adjacent sequences in a chain-folded polymer.21 The crystal structure of [82+1] thus provides a clear-cut demonstration of the chain-folding-and-adjacent-binding proposed for detection of long-range sequence information by tweezer-molecules 6, 7, and 8.

Figure 3 (  Job plots for complexation of 8 (((()  and 9 (––) with the bis(diimide) oligomer 2, based on 1H NMR complexation shifts of the aromatic diimide resonances. Samples were 6 mM in total concentration. Peak abscissa values of 0.32 and 0.48 indicate 2:1 (tweezer: oligomer) and 1:1 complexation respectively.

Confirmation that the adjacent tweezer-binding observed in the crystal can also occur in solution was provided by Job plots for complexation of tweezer-molecule 8 with oligo-imides 1 and 2 in chloroform/hexafluoropropan-2-ol, using the complexation shifts () of the singlet diimide resonance in each case. These plots provide very good evidence for 2:1 (tweezer:oligomer) stoichiometry of binding, with peaks found at x = 0.39 and 0.32 respectively (c.f.  theoretical values of 0.33 for 2:1 and 0.50 for 1:1 binding). Remarkably however, Job analyses of complexation between the internally hydrogen-bonded tweezer 9 and oligomers 1 and 2 showed a clear-cut preference for one-to-one binding, with the latter plots peaking at x = 0.50 and 0.48 respectively (Fig. 3). The 2:1 tweezer-oligomer binding model established from the structure of complex [82+1] (Fig. 2) thus fails completely for tweezer-molecule 9. However, computational modelling (molecular mechanics with charge-equilibration) quickly showed that 1:1 complexation between tweezer-molecule 9 and diimide oligomers 1 and 2 could be accounted for in terms of tweezer-binding at the 4,4'-biphenylenedisulfone unit of the oligomer (Fig. 4a). This gives rise to a five-component, complementary -stack in which the diimide residues interact with the outer faces of the tweezer-arms, rather than with their inner faces as in complex [82+1] (Fig. 2).

Figure 4 (  Minimised computational models (molecular mechanics with charge-equilibration) of (a) the 1:1 complex between tweezer-molecule 9 and the bis-pyromellitimide oligomer 1, and (b) the 2:1 complex between tweezer-molecule 9 and the tris-diimide oligomer 3. Intramolecular hydrogen bonds are shown in magenta. In complex [92+3] the two tweezer-molecules are shown approaching from opposite sides of the oligomer chain, though the system is dynamic and simultaneously-complexed tweezer-molecules could in fact be bound syn or anti to one another. Van der Waals surfaces are shown at 2.4 x covalent radii.

A closely-related structure was found, computationally, for the complex between the tris-diimide oligomer 3 and tweezer-molecule 9 (Fig. 4b), where two molecules of the tweezer bind at consecutive, biphenylene-centred "ISI" sequences. This model leads to the prediction that the 1H NMR resonances of oligomer 3 associated with the biphenylene units and the central diimide residue (all of which are shielded by two tweezer-pyrenyl groups) should show significantly greater complexation shifts () with tweezer 9 than those arising from the terminal diimide groups, which are shielded by only a single pyrene unit. As shown in Fig. 5, this prediction is borne out in practice, with values (2:1 mole ratio of tweezer-molecule 9 to the tris-diimide oligomer 3) of 0.23 and 0.24 ppm for protons Ha and Hb/b' contrasting with a  value of only 0.14 ppm for the AB system representing the protons (Hd/e) of the terminal diimide units. The spectra shown in Fig. 5 were obtained at 50 °C (fast exchange conditions) since room-temperature spectra were significantly broadened, suggesting an approach to slow exchange between bound and unbound species.

The different sequence-selectivities of tweezer molecules 8 (SIS) and 9 (ISI) may be accounted for on the basis of their different hydrogen-bonding characteristics. Historically, tweezer-type molecules have invariably been found to bind small aromatic guests by a mechanism analogous to chelation in coordination chemistry, i.e. by using the inner surfaces of their tweezer-arms.10-16 However, when the "guest" molecule is a chain-folding oligomer or polymer, it is entirely feasible that – depending on the detailed geometrical parameters and conformational flexibility of the tweezer – -stacking of the diimide residues to the outer faces of the tweezer-arms could be preferred. Energetically, it makes no difference which face of the pyrenyl residue interacts with the diimide. Indeed, in the absence of other types of interaction, outer-face complexation might even be the norm, and it is clearly favoured for the intramolecularly hydrogen-bonded diester-tweezer 9 (Figs. 4, 5 and 6), leading to complexation at the sequence "ISI". In contrast, the diamide tweezer-molecule 8 and analogues such as 6 and 7 have two convergent N-H groups, each of which can form an intermolecular hydrogen bond to the carbonyl group of a diimide residue in a poly- or oligo-imide chain (Fig. 2). This would obviously promote tweezer-binding at the diimide unit, now leading to complementary --stacking between the diimide ring and the inner surfaces of the tweezer-arms. As a result, the diamide-type tweezers invariably show selective binding at the sequence "SIS".19,20,21

Figure 5 (  1H NMR spectra showing complexation shifts of different resonances for the tris-diimide oligomer 3 (lower trace) in the presence of tweezer-molecule 9, at 1:1 (centre trace) and 1:2 (upper trace) molar ratios respectively. Spectra were run at 500 MHz in CDCl3/hexafluoropropan-2-ol (6:1 v/v) at 50 °C, at 2 mM total concentration.

We were unable to isolate diffraction-quality crystals of the proposed 1:1 oligo-imide complex [1+9] but the modelled biphenylene-centred binding mode was indeed identified for tweezer-molecule 9 by a single crystal X-ray study of the 1:1 complex between 9 and an analogous macrocyclic oligo-imide 11. Here, in contrast to all previous tweezer-diimide assemblies for which structural data are available,19,20,21, the imide unit of 11 does not represent the central binding site for the tweezer-molecule, which instead binds  at the 4,4'-biphenylene-disulfone unit. However, as with tweezer-molecule 6, where binding to macrocycle 11 occurs at the diimide residue,43 the new macrocycle-tweezer complex [9+11] packs to generate an "infinite", complementary stack in which -electron-deficient diimide residues alternate with -electron-rich pyrenyl units (Fig. 6).

Conceptually, ring-opening polymerisation of the macrocycles in such an infinite stack would generate a tweezer-bound, chain-folded homopolymer, with the tweezer-molecules located on the 4,4'-biphenylenedisulfone units ("S"). The diimide residues ("I") would again stack onto the outer surfaces of the tweezer-arms. The structure of [9+11] thus confirms that, in a chain-folded polymer, tweezer 9 favours binding to the sequence "ISI", rather than to "SIS". Moreover, further analysis shows that this particular sequence-selectivity provides an immediate explanation for the exceptional power of 9 to reveal long-range sequence information in the 1H NMR spectra of high-MW copolyimides.22

Figure 6 (  X-ray structure of the complex between macrocycle 11 and tweezer-molecule 9, showing molecular stacking along the crystallographic a-direction. Tweezer-molecules are shown in blue, emphasising the alternation of complementary donor (pyrenyl) and acceptor (diimide and biphenylenedisulfone) subunits in the -stack. Intramolecular hydrogen bonds (N-H…O=C) are shown in magenta. The tweezer-molecule clearly binds at the 4,4'-biphenylenedisulfone site, but the outer faces of its arms are both able to -stack, in the crystal, with strongly electron-accepting diimide units.

Consider the 1:1 copolymer 13, in which the hexafluoroisopropylidene-diphthalimide groups generate entirely non-tweezer-binding sequences. Here the steric bulk of the hexafluoroisopropylidene unit and the twisted orientation of the two connected phthalimide groups combine to ensure that direct tweezer-binding cannot take place at this residue. Specifying the pyromellitimide unit as "I", the hexafluoroisopropylidene-diphthalimide group as "F", and the biphenylene-disulfonyl-diamine residue as "S", the allowed septet sequences in this copolymer (centring on the pyromellitimide unit observed by 1H NMR) are then:  [–SISISIS–], [–SFSISIS– or –SISISFS–], and [–SFSISFS–]. The structure of complex [82+1] reported here, together with previous spectroscopic studies,21 establishes that these sequences can bind three, two and one tweezer-molecules of type 8 respectively at their SIS triplet sequences (note: the "S" units are shared or "overlapping" under this terminology). Tweezer-binding at SIS results in large upfield shifts (> 2.5 ppm) for the central diimide resonance in each case, but additional shielding from adjacently bound tweezer(s) present produces further (small) complexation shifts, so resolving a different diimide resonance for each different septet sequence. The key point is that the central diimide residue can bind a molecule of type 8 in all three sequences of this type (Table 1).

Conversely, tweezer 9 binds predominantly at the sequence "ISI" and only very weakly, if at all, at the directionally-degenerate sequences FSI and ISF. As a result, the central diimide protons of the septet sequences are now much more sharply differentiated in terms of their susceptibility to ring-current shielding by complexing tweezer-molecules. As shown for 9 in Table 1, two tweezer molecules bind to [–SISISIS–], one to [–SFSISIS– or –SISISFS–], and none at all to [–SFSISFS–]. Consequently, interaction with 9 means that the central diimide residues in these septet sequences are shielded directly by two, one and no pyrenyl units respectively. This is a very different situation from that described for complexation of 8 to the same sequences, where the central, "observed" diimide protons are shielded directly by two pyrenyl residues in all cases. The novel sequence-selectivity discovered in this work for tweezer-molecule 9 (i.e. "ISI" rather than "SIS") thus provides a simple explanation for the extraordinarily high sensitivity to this tweezer of 1H NMR resonances associated with long-range sequence-information.22 Conversely, the "anomalous" behaviour of copolyimide 1H NMR resonances in the presence of tweezer-molecule 9 can now be seen, in conjunction with Table 1, to provide strong evidence that this molecule does indeed display a general preference for binding to the triplet sequence "ISI", rather than "SIS".

Table 1 (  Graphical representation of "frameshift" reading resulting from the different sequence-recognition characteristics of tweezer-molecules 6, 7, 8 and 9.  The "observed" protons at the central diimide unit (I) in the first sequence are shielded to a similar extent by the pyrenyl residues of both tweezers (two proximal and two distal pyrenes). However, with tweezer-molecule 9, the presence of a non-binding hexafluoroisopropylidene-diimide (F) unit at one or both adjacent sites has a more drastic effect on the number of pyrenes shielding the diimide protons. As a result, the chemical shifts of ther three sequences are much more strongly differentiated through ring-current shielding in the presence of 9 than of 6, 7 or 8.

In reality the situation is not quite so clear-cut, because even the diimide resonance arising from the "non-9-binding" sequence [–SFSISFS–] does undergo a small upfield shift in the presence of this tweezer. It is already known that 9 can bind weakly to a diimide residue,22 and since the NMR experiments described here all show fast exchange between bound and unbound tweezer-molecules, it seems that the strong "ISI" complexation proposed for tweezer 9 will be dynamically superimposed on much weaker "SIS" binding, with both mechanisms operating simultaneously on the NMR timescale. Consistent with this, the 1:1 association constant, Ka, measured (using the UV-visible dilution method, based on the charge-transfer band at 551 nm) for the binding of tweezer-molecule 9 to the chain-folding oligomer 2, was found in this work to be 780 M-1, more than five times higher than the value (140 M-1)22 of Ka for the binding of 9 to the simple diimide 10. In the context of this 500% increase in binding constant, it should be noted that the experimental error in binding constants determined by the UV-vis. dilution method is normally of the order of 15%.

We have thus established, through studies of fully-defined oligomers and their tweezer-complexes, that two different designs of tweezer-molecule (exemplified by 8 and 9) have structures which are complementary to two different triplet-sequences in chain-folding polyimide-sulfones. This situation is faintly reminiscent of the relationship between the different t-RNA's (each having a different "binding codon") and m-RNA. Correspondingly, homopolyimide 12 can be represented as the sequence ...SISISISISIS..., with tweezer-molecules 6, 7 and 8 binding to the triplets "SIS", while the present work shows that tweezer-molecule 9 binds preferentially to the  sequence "ISI", so that the "reading frame" for 9 can be thought of as being shifted to left or right by a single monomer residue (Fig. 7).

Figure 7 (  Chain folding and multiple binding to different polyimide triplet-sequences by different tweezer-molecules.  Defining the diarylpyromellitimide unit as "I" and the bis(arylsulfonyl)biphenylene residue as "S", each tweezer-molecule binds either to monomer-sequence "SIS" (tweezer 6, upper) or to ISI (tweezer 9, lower). Note: following the frameshift, the right-hand tweezer molecule in the lower arrangement is too distant from the "observed" protons (shown in blue) to play any role in ring-current shielding.

Acknowledgements

This research was supported by EPSRC (grants EP/C533526/1, EP/E00413X/1, EP/F013663/1 and EP/G026203/1) and by the Royal Society (a Senior Research Fellowship to HMC).

Author contributions

Z.Z. and H.M.C. designed the synthetic and spectroscopic experiments and interpreted the resulting data. Z.Z. carried out the experiments and co-wrote the paper. C.J.C. and Y.G. undertook the crystallographic work, including structure solution, refinement and data-analysis. H.M.C. conceived and supervised the project, generated the graphics, and wrote the paper.

Additional information

Supplementary information, including full synthetic, analytical, spectroscopic and crystallographic data, accompanies this paper at w.w.w.nature.com/naturechemistry. Reprints and permissions information are available online at http://npg.nature.com/reprints and permissions/. Correspondence and requests for materials should be addressed to H.M.C.

References

# Endnotes

Watson, J. D. & Crick, F. H. C. A structure for deoxyribose nucleic acid. Nature 	171, 737-738 (1953).

Wilkins, M. H. F., Stokes, A. R. & Wilson, H. R. Molecular structure of 	deoxypentose nucleic acids. Nature 171, 738-740 (1953).

Franklin R. E. & Gosling, R. G. Molecular configuration in sodium thymonucleate. 	Nature 171, 740-741 (1953).

Crick, F. H. C. On protein synthesis. Symp. Soc. Exptl. Biol. 12, 138-163 (1958).

Nirenberg, M. Deciphering the genetic code - a personal account. Trends Biochem. 	Sci. 29, 46-54 (2004).

Dawkins, C. R. The Blind Watchmaker, Longmans, London, 1986.

Lodish, H., et al. Molecular Cell Biology, Freeman, New York, 6th Edn., 2007.

Burd, C. & Weck, M. Self-sorting in polymers. Macromolecules, 38, 7225-7230 	(2005).

Weck, M. Side-chain functionalized supramolecular polymers. Polym. Int. 56, 453-	460 (2007).

Harmata, M. Chiral molecular tweezers. Acc. Chem. Res. 37, 862-873 (2004).

Klärner, F-G. & Kahlert, B. Molecular tweezers and clips as synthetic receptors. 	Molecular recognition and dynamics in receptor-substrate complexes. Acc. Chem. 	Res. 36,  919-932 (2003).

Chen, C. W. & Whitlock, H. W. Molecular tweezers - a simple model of 	bifunctional intercalation. J. Am. Chem. Soc. 100, 4921 (1978).

Zimmerman, S. C. & VanZyl, C.M. Rigid molecular tweezers - synthesis, 	characterization, and complexation chemistry of a diacridine. J. Am. Chem. Soc. 	109, 7894-7896 (1987).

Kurebayashi, H., Haino, T., Usui, S. & Fukazawa, Y. Structure of 	supramolecular 	complex of flexible molecular tweezers and planar guest in 	solution. Tetrahedron, 	57, 8667-8674 (2001).

Balzani, V. et al. Host-guest complexes between an aromatic molecular tweezer 	and symmetric and unsymmetric dendrimers with a 4,4 '-bipyridinium core. J. Am. 	Chem. Soc. 128, 637-648 (2006).

Klärner, F-G., et al. Molecular tweezer and clip in aqueous 	solution: Unexpected 	self-assembly, powerful host-guest complex formation, quantum chemical H-1 	NMR shift calculation. J. Am. Chem. Soc. 128, 4831-4841 (2006).

Goshe, A. J., Steele, I. M., Ceccarelli, C., Rheingold, A.L. & Bosnich, B. 	Supramolecular recognition: On the kinetic lability of thermodynamically stable 	host-guest association complexes. Proc. Acad. Sci. U.S.A. 99, 4823-4829 (2002).

Peng, X-X., Lu, H-Y., Han, T. & Chen, C-F. Synthesis of a novel triptycene-based 	molecular tweezer and its complexation with paraquat derivatives. 	Org. Lett. 9, 	895-898 (2007).

Colquhoun, H. M. & Zhu, Z. Recognition of polyimide sequence information by a 	molecular tweezer. Angew. Chem., Int. Ed. 43, 5040-5045 (2004).

Colquhoun, H. M., Zhu, Z., Cardin C. J. & Gan, Y. Principles of sequence-	recognition in aromatic polyimides. Chem. Commun., 2650-2652 (2004).

Colquhoun, H. M., Zhu, Z., Cardin, C. J., Gan Y. & Drew, M. G. B. Sterically 	controlled recognition of macromolecular sequence information by molecular 	tweezers. J. Am. Chem. Soc. 129, 16163-16174 (2007).

Colquhoun, H. M., Zhu, Z., Cardin, C. J., Drew, M. G. B. & Gan, Y. Recognition 	of sequence-information in synthetic copolymer chains by a conformationally-	constrained tweezer molecule. Faraday Discuss., 143, 205-220 (2009).

Hamilton, D. G., Sanders, J. K. M., Davies, J. E., Clegg, W. & Teat, S. J. Neutral 	[2]catenanes from oxidative coupling of -stacked components. Chem. Commun. 	897-898 (1997).

Hamilton, D. G., Lynch, D. E., Byriel,  K. A., Kennard C. H. L. & Sanders, J. K. 	M. N-alkylation of pyromellitic diimide: Solid-state structure of the 1:1 N,N'-	diethylpyromellitic diimide 2,6-dimethoxynaphthalene cocrystal. Aust. J. Chem. 51, 	441-444 (1998).

Hamilton, D. G., Davies, J. E., Prodi, L. & Sanders, J. K. M. Synthesis, structure 	and photophysics of neutral -associated [2]catenanes. Chem. Eur. J. 4, 608-620 	(1998).

Hamilton, D. G., Feeder, N., Teat S. J. & Sanders, J. K. M. Reversible 	synthesis of -associated [2]catenanes by ring-closing metathesis: towards dynamic 	combinatorial libraries of catenanes New J. Chem. 1019-1021 (1998).

Kaiser, G., et al. Lithium-templated synthesis of a donor-acceptor pseudorotaxane 	and catenane. Angew. Chem., Int. Ed., 43, 1959-1962 (2004).

Vignon, S. A., et al. Switchable neutral bistable rotaxanes. J. Am. Chem. Soc., 126, 	9884-9885 (2004).

Iijima, T. et al. Controllable donor-acceptor neutral [2]rotaxanes. Chem. Eur. J. 	10, 6375-6392 (2004).

Pascu S. I. et al. Cation-reinforced donor-acceptor pseudorotaxanes. New J. Chem. 	80-89 (2005).

Hansen, J. G., Bang, K. S., Thorup N., & Becher, J. Donor-acceptor macrocycles 	incorporating tetrathiafulvalene and pyromellitic diimide: Syntheses and crystal 	structures. Eur. J. Org. Chem. 2135-2144 (2000).

Colquhoun, H. M., Stoddart, J. F., Williams, D. J., Wolstenholme J. B. & 	Zarzycki, R. Second-sphere coordination of cationic platinum complexes by crown 	ethers - the X-ray crystal-structure of [Pt(bpy)(NH3)2.Dibenzo[30]crown-	10]2+[PF6]–2.xH2O (x = 0.6). Angew. Chem., Int. Ed. Engl. 20, 1051-1053 (1981).

Colquhoun, H. M. et al. Complex-formation between dibenzo-3n-crown-n ethers 	and the diquat dication. J. Chem. Soc., Chem. Commun., 1140-1142 (1983).

Allwood, B. L., Spencer, N., Shahriari-Zavareh, H., Stoddart, J. F. & Williams, D. 	J. Complexation of diquat by a bisparaphenylene-34-crown-10 derivative. J. Chem. 	Soc., Chem. Commun. 1061-1064 (1987).

Ashton, P. R., Slawin,  A. M. Z., Spencer, N., Stoddart, J. F. & Williams, D. J. 	Complex formation between bisparaphenylene-(3n+4)-crown-n ethers and the 	paraquat and diquat dications. J. Chem. Soc., Chem. Commun. 1066-1069 (1987).

Krebs, F. C. & Jørgensen, M. A new versatile receptor platform. J. Org. Chem. 66, 	6169-6173 (2001).

Koshkakaryan, G. et al. Alternative donor-acceptor stacks from crown ethers and 	naphthalene diimide derivatives: rapid, selective formation from solution and 	solid state grinding. J. Am. Chem. Soc. 131, 2078-2079 (2009).

Peinador, C., Blanco V. & Quintela, J. A new doubly interlocked [2]catenane. J. 	Am. Chem. Soc. 131, 920-921 (2009).

Ulrich, S. & Lehn, J. M. Adaptation and optical signal generation in a constitutional 	dynamic network. Chem. Eur. J., 15, 	5640-5645 (2009).

Lohr, A., Grüne, M. & Würthner, F. Self-assembly of bis(merocyanine) tweezers 	into discrete bimolecular -stacks. Chem. Eur. J. 15, 3691-3705 (2009).

Harris, F. W. in Polyimides, Wilson, D., Stenzenberger H. D. & Hergenrother, P. 	M. (Eds.), Chapman and Hall, New York, 1990, Chapter 1.

Klod, S. & Kleinpeter, E. Ab initio calculation of the anisotropy effect of multiple 	bonds and the ring current effect of arenes - application in conformational and 	configurational analysis. J. Chem. Soc., Perkin Trans. 1893-1898 (2001).

Colquhoun, H. M., Zhu, Z. & Williams, D. J. Extreme complementarity in a 	macrocycle-tweezer complex. Org. Lett. 5, 4353-4356 (2003).

Nielsen, M. B. et al., Binding studies between tetrathiafulvalene derivatives and

cyclobis(paraquat-p-phenylene). J. Org. Chem. 66, 3559-3563 (2001).

Johnson, Z. I. & Chisholm, S. W. Properties of overlapping genes are conserved 	across microbial genomes. Genome Res. 14, 2268-2272 (2004).